|  | Idaho Microfabrication Laboratory |
| --- | --- |

Spin Coater Recipes

Do not change any recipes below except those designated to your group or the OPEN recipe.

| Recipes |  |  | Step 1 |  |  | Step 2 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| # | Group | Purpose | Time (sec) | Speed (RPM) | Ramp (RPM/sec) | Time (sec) | Speed (RPM) | Ramp (RPM/sec) |
| 1 | General | HMDS | 5 | 500 | 1000 | 35 | 5000 | 1000 |
| 2 | General | 1um (SPR 220-1.2) 6um (SPR 220-7.0) | 30 | 3500 | 2000 | 0 | 0 | 0 |
| 3 | DARPA | PR (SPR 220-7.0) | 5 | 500 | 500 | 35 | 3500 | 500 |
| 4 | DARPA |  |  |  |  |  |  |  |
| 5 | Jessing | 9um (SPR 220-7.0) | 5 | 500 | 1000 | 30 | 2500 | 500 |
| 6 | Jessing |  |  |  |  |  |  |  |
| 7 | Jozwiak |  |  |  |  |  |  |  |
| 8 | EBL | 0.3um PMMA | 5 | 500 | 500 | 45 | 3500 | 1000 |
| 9 | OPEN* | OPEN* | -- | -- | -- | -- | -- | -- |

*Recipe # can be changed at each use by anyone on the qualified users list.